## Slide 1: Zintl-Based Materials For Thermoelectrics
286G Final Presentation, 5-26-2010
Brett Compton
Ca11GaSb9

## Slide 2
Thermoelectric Concept
Snyder and Toberer, 2008
Bell, 2008

## Slide 3
Material Property Requirements
Dimensionless Figure of Merit:
Seebeck Coefficient:
Electrical Conductivity:
Thermal Conductivity:
Electronic Contribution
to Thermal Conductivity:
Effective TE materials need tunable carrier concentrations
and low lattice thermal conductivity: “Electron crystal – phonon glass”
Snyder and Toberer, 2008

## Slide 4
What Are Zintl Materials?
Valence balanced intermetallic compounds
with ionic and covalent bonding character.
Nesper, 1990
1. Typically: AXs A: Group 1 or 2 metal
X: Semi-metal
2. Semiconducting
3. Diamagnetic
4. X – X bonding
Zintl-Klemm Concept:
There is complete charge transfer from
A to the Xs “Zintl anion.”
The Zintl anions then form bonds to
satisfy valence.

## Slide 5
Simple Zintl Phase: NaTl
Ionic bonding results in
Na+ Tl-
[Tl-] has 4 valence electrons and
forms a covalent diamond structure
with the Na+ cations stuffing the
lattice.
The covalent network in Zintl materials provides the “electron crystal”
properties while the cation sites allow for carrier concentration tuning
and phonon scattering.

## Slide 6
A More Complicated Example: CaZn2Sb2
Ca2+ [Zn2Sb2]2-
Ca is rather electropositive and donates two electrons to the
[Zn2Sb2] unit. [Zn2Sb2]2- is isoelectronic with ZnS and forms a
wurtzite-like structure with intercalated Ca2+ sheets.
This is a semiconductor with a band gap of 0.25 eV.
Kauzlarich et al., 2007
Ca
Sb
Zn
Wurtzite
Notes: Similar to Wurtzite structure with Ca2+ layers intercalated in.

## Slide 7
Tuning CaZn2Sb2 For Thermoelectric Properties
CaxYb1-x
Sb
Zn
Alloy Isoelectronic Species: Yb for Ca
(CaxYb1-x)2- [Zn2Sb2]2+
Gascoin et al., 2005
Yb is less electropositive than Ca which results in an incomplete
charge transfer to [Zn2Sb2]2- and therefore high p-type carrier
concentration in the anionic lattice.

## Slide 8
Tuning CaZn2Sb2 For Thermoelectric Properties
CaxYb1-x
Sb
Zn
Alloy Isoelectronic Species: Yb for Ca
(CaxYb1-x)2- [Zn2Sb2]2+
Toberer et al., 2009
Additionally, Yb is much heavier than Ca (~4:1) which results in effective
phonon scattering and significantly reduced thermal conductivity.

## Slide 9
Tuning CaZn2Sb2 For Thermoelectric Properties
CaxYb1-x
Sb
Zn
Alloy Isoelectronic Species: Yb for Ca
(CaxYb1-x)2- [Zn2Sb2]2+
Gascoin et al., 2005
The combination of carrier concentration tuning and phonon scattering
can result in a significant improvement in zT for this material.

## Slide 10
Other Zintl-based Thermoelectrics
Skutterudite: CoSb3
Snyder and Toberer, 2008
14-1-11: Yb14MnSb11
Kauzlarich et al., 2007
Filled

## Slide 11
Bell, L. E. (2008). Cooling, heating, generating power, and recovering waste heat with thermoelectric systems. Science (New York, N.Y.), 321(5895), 1457-61. doi: 10.1126/science.1158899.
Gascoin, F., Ottensmann, S., Stark, D., Haïle, S. M., & Snyder, G. J. (2005). Zintl Phases as Thermoelectric Materials: Tuned Transport Properties of the Compounds CaxYb1-xZn2Sb2. Advanced Functional Materials, 15(11), 1860-1864. doi: 10.1002/adfm.200500043.
Kauzlarich, S. M., Brown, S. R., & Snyder, G. J. (2007). Zintl phases for thermoelectric devices. Dalton transactions (Cambridge, England : 2003), (21), 2099-107. doi: 10.1039/b702266b.
Nesper, R. (1990). Structure and chemical bonding in zintl-phases containing lithium. Progress in Solid State Chemistry, 20(1), 1-45. doi: 10.1016/0079-6786(90)90006-2.
Sales, B. C., Jin, R., & Mandrus, D. (2008). Zintl Compounds : From Power Generation To The Anomalous Hall Effect. Quantum, (Skutterudite 2007), 48-53.
Snyder, G. J., & Toberer, E. S. (2008). Complex thermoelectric materials. Nature materials, 7(2), 105-14. doi: 10.1038/nmat2090.
Toberer, E. S., May, A. F., & Snyder, G. J. (2010). Zintl Chemistry for Designing High Efficiency Thermoelectric Materials † ‡. Chemistry of Materials, 22(3), 624-634. doi: 10.1021/cm901956r.
References