## Slide 1: Cu(I) based delafossites as candidate materials for p-type transparent conducting oxides
05/28/10
Roy Rotstein

## Slide 2: ITO widely used in electronic devices

## Slide 4: Considerations for p-type TCO
Positive charges (holes) act as charge carriers
Bandgap must be greater than 3eV to avoid absorption in the visible spectrum
Localization of upper edge of valence band to oxides results in low hole mobility

## Slide 5: Structural characteristics of CuMO2 delafossites
Gabriel Delafosse
M3+
Cu(I)
oxygen
Space Group: R3m

## Slide 6: Rational design of a p-type delafossite TCO
Covalent bonding behavior between cation and oxide helps reduce localization of 2p electrons from oxide
Cation must have a closed electronic shell
  Avoid coloration from intra-atomic excitation
  Energy level must be comparable to 2p electrons from oxides

## Slide 7: CuAlO2 optically transparent
Kawazoe, Hiroshi; et al. "P-type Electrical Conduction in Transparent Thin Films of CuAlO2." Nature 389 (1997): 939-42.
Estimated Eg = 3.5 eV
Film thickness: 500nm

## Slide 8: CuAlO2 exhibits semiconductive temperature dependence
Conductivity at room temperature: 0.095 S/cm
Carrier density: 1.3 * 1017 cm-3
Hole mobility: 10.4 cm2-V1s-1
Seebeck coefficient: 183μVK-1

## Slide 9: Doping with divalent cations increases conductivity
Nagarajan, R., A. D. Draeseke, A. W. Sleight, and J. Tate. "P-type Conductivity in CuCr1-xMgxO2 Films and Powders." Journal of Applied Physics 89.12 (2001): 8022-025.
Film Thickness: 250nm
Conductivity at
room temperature: 200 S cm-1

## Slide 10: Annealing at 900°C increases transparency but reduces conductivity
Pre-annealing: 200 S cm-1
Post-annealing: 1 S cm-1

## Slide 11: Conclusions
Cu(I) based delafossites are the leading candidate materials for p-type TCO
Origin of p-type behavior unkown for undoped compounds
Tradeoff between transparency and conductivity in doped compounds