## Slide 1: Off-centering Distortions in Thermoelectrics
Jonathon Bechtel
May 28, 2014

## Slide 4: Basic Working Principles
Seebeck Effect.
Figure of Merit:
Conflicting material requirements.
DiSalvo, Francis J. "Thermoelectric cooling and power generation." Science 285, no. 5428 (1999): 703-706.

## Slide 5: Approaches to low lattice thermal conductivity, κL
Umklapp Scattering
Introduce disorder through Point Defects/Nanostructuring
Complex/Large Unit Cells
Rattling Atoms
Toberer, Eric S., Alex Zevalkink, and G. Jeffrey Snyder. "Phonon engineering through crystal chemistry." Journal of Materials Chemistry 21, no. 40 (2011): 15843-15852.
ˆ

## Slide 6: Phonon Conduction
Mass Contrast
Complex Unit Cell
Toberer, Eric S., Lauryn L. Baranowski, and Chris Dames. "Advances in thermal conductivity." Annual Review of Materials Research 42 (2012): 179-209.
Toberer, Eric S., Alex Zevalkink, and G. Jeffrey Snyder. "Phonon engineering through crystal chemistry." Journal of Materials Chemistry 21, no. 40 (2011): 15843-15852.

## Slide 7: Guest atom inclusion to promote rattling modes.
Rattling
Avoided Crossing
  Reduced group velocity
Toberer, Eric S., Lauryn L. Baranowski, and Chris Dames. "Advances in thermal conductivity." Annual Review of Materials Research 42 (2012): 179-209.
Toberer, Eric S., Alex Zevalkink, and G. Jeffrey Snyder. "Phonon engineering through crystal chemistry." Journal of Materials Chemistry 21, no. 40 (2011): 15843-15852.

## Slide 8: Clathrate host-guest structure promotes rattling modes
Ba8Ga16Ge30
Christensen, Mogens, et. al. "Avoided crossing of rattler modes in thermoelectric materials." Nature materials 7, no. 10 (2008): 811-815.

## Slide 9: Reconsider simple rock-salt thermoelectric materials
Moderate mass contrast
Cubic rock-salt unit cell
How to explain low κL?
Toberer, Eric S., Alex Zevalkink, and G. Jeffrey Snyder. "Phonon engineering through crystal chemistry." Journal of Materials Chemistry 21, no. 40 (2011): 15843-15852.

## Slide 10: Reconsider simple rock-salt thermoelectric materials
Early evidence of off-centering upon heating
  Asymmetric nearest neighbor peak.
Disordered, off-center cations
Božin, Emil S., Christos D. Malliakas, Petros Souvatzis, Thomas Proffen, Nicola A. Spaldin, Mercouri G. Kanatzidis, and Simon JL Billinge. "Entropically stabilized local dipole formation in lead chalcogenides." Science 330, no. 6011 (2010): 1660-1663.

## Slide 11: Further evidence of off-centering
Kastbjerg, Sofie, Niels Bindzus, Martin Søndergaard, Simon Johnsen, Nina Lock, Mogens Christensen, Masaki Takata, Mark A. Spackman, and Bo Brummerstedt Iversen. "Direct Evidence of Cation Disorder in Thermoelectric Lead Chalcogenides PbTe and PbS." Advanced Functional Materials 23, no. 44 (2013): 5477-5483.
SPXRD to quantify cation disorder
Maximum entropy method for electron densities
Confirm off-centering

## Slide 12: Rationalize unusual behavior with simple thermodynamic argument
F = U – T*S
Metastable state entropically stabilized at high temperature
Božin, Emil S., Christos D. Malliakas, Petros Souvatzis, Thomas Proffen, Nicola A. Spaldin, Mercouri G. Kanatzidis, and Simon JL Billinge. "Entropically stabilized local dipole formation in lead chalcogenides." Science 330, no. 6011 (2010): 1660-1663.

## Slide 13: Departure from Landau Theory
Opposite of traditional phase transition
Fluctuating dipoles may affect:
  Thermal conductivity, carrier mobility (T-2.5)
Božin, Emil S., Christos D. Malliakas, Petros Souvatzis, Thomas Proffen, Nicola A. Spaldin, Mercouri G. Kanatzidis, and Simon JL Billinge. "Entropically stabilized local dipole formation in lead chalcogenides." Science 330, no. 6011 (2010): 1660-1663.

## Slide 14: PbTe phonon dispersion reveals avoided crossing
Highly anharmonic phonon coupling
  LA vs. TO
Scattering
  LA+TO <-> LO
Incipient Ferroelectric
  Waterfall effect
Delaire, Olivier, Jie Ma, Karol Marty, Andrew F. May, Michael A. McGuire, Mao-Hua Du, David J. Singh et al. "Giant anharmonic phonon scattering in PbTe." Nature materials 10, no. 8 (2011): 614-619.

## Slide 15: Emphanisis in SnTe
Knox, K. R., E. S. Bozin, C. D. Malliakas, M. G. Kanatzidis, and S. J. L. Billinge. "Local off-centering symmetry breaking in the high-temperature regime of SnTe." Physical Review B 89, no. 1 (2014): 014102.
SnTe: Rhombohedral to Cubic to Emphanitic

## Slide 16: Conclusions and Outlooks
Avenues to low κL
Phonon Engineering
Off-centering
Emphanisis and Lone Pairs
Božin, Emil S., Christos D. Malliakas, Petros Souvatzis, Thomas Proffen, Nicola A. Spaldin, Mercouri G. Kanatzidis, and Simon JL Billinge. "Entropically stabilized local dipole formation in lead chalcogenides." Science 330, no. 6011 (2010): 1660-1663.