## Slide 1
How transition metal, anion, and structure
affect the operating potential of an electrode
Megan Butala
June 2, 2014

## Slide 2
Hayner, Zhao & Kung. Annu .Rev. Chem. Biomolec. Eng. 3, 445–71 (2012).
A wide range of electrode potentials
can be achieved
Notes: Can see variation with TM, anion, oxidation state

## Slide 3
Power and energy are common metrics
for comparing energy storage technologies
Hayner, Zhao & Kung. Annu .Rev. Chem. Biomolec. Eng. 3, 445–71 (2012).
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 4
What physical phenomena
are described by these metrics?
Specific energy = capacity × Voc
Specific power = Specific energy × time to charge
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 5
What physical phenomena
are described by these metrics?
Specific energy = capacity × Voc
Specific power = Specific energy × time to charge
charge stored per mass active material
xLi+ +xe-+ Li1-xCoO2
LiCoO2
Ex:
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 6
What physical phenomena
are described by these metrics?
Specific energy = capacity × Voc
Specific power = Specific energy × time to charge
charge stored per mass active material
Voc = (μA – μC)/e
Voc = EMFC - EMFA
xLi+ +xe-+ Li1-xCoO2
LiCoO2
Ex:
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 7
How a battery works
V and chemical potential
Batteries by DOS
Notes: Turn this schematic image over, think about

## Slide 8
How a battery works
V and chemical potential
Batteries by DOS
Notes: Turn this schematic image over, think about

## Slide 9
Anode
Cathode
Li+ ions and electrons are shuttled between electrodes to store and deliver energy
Notes: On discharge – reducing cathode (Li to cathode)
Improve title

## Slide 10
Anode
Cathode
e-
Li+
Li+
Applying a load to the cell drives Li+ and electrons to the cathode during discharge
Notes: On discharge – reducing cathode (Li to cathode)

## Slide 11
Anode
Cathode
e-
Li+
Li+
V
Applying a voltage to the cell drives Li+ ions and electrons to the anode during charge
Notes: On discharge – reducing cathode (Li to cathode)

## Slide 12
How a battery works
V and chemical potential
Batteries by DOS
Notes: Turn this schematic image over, think about

## Slide 13
We can consider the energies of
the 3 major battery components
Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
eVoc = μA - μC
Voc = EMFC - EMFA
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 14
We can consider the energies of
the 3 major battery components
Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
eVoc = μA - μC
Voc = EMFC - EMFA
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 15
An electrode’s EMF can be understood
by the nature of its DOS
Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 16
An electrode’s EMF can be understood
by the nature of its DOS
Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
Lower orbital energy = higher potential
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 17
How a battery works
V and chemical potential
Batteries by DOS
Notes: Turn this schematic image over, think about

## Slide 18
The potential of an electrode depends on chemistry and structure
MaXb
M = transition metal
X = anion (O, S, F, N)
X p-band
M dn+1/dn
M dn/dn-1
E
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 19
Transition metal energy stabilization shows trends from L to R based on ionization energy
Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 20
Transition metal energy stabilization shows trends from L to R based on ionization energy
Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
Ti
Co
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 21
Transition metal energy stabilization shows trends from L to R based on ionization energy
Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
Ti
Co
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 22
Adapted from Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
S p-band
O p-band
F p-band
E
The relative stabilization and bandwidth of the anion (X) p-band vary with electronegativity
EN ↑
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 23
The relative stabilization and bandwidth of the anion (X) p-band vary with electronegativity
Adapted from Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
S p-band
O p-band
F p-band
E
BW
EN ↑
Notes: Bandwidth of d bands also decrease with increasing EN of anion

## Slide 24
MaXb
X p-band
M dn+1/dn
M dn/dn-1
E
U
Δ
Mott-Hubbard vs. charge transfer dominated character will alter potential
Zaanen, Sawatzky & Allen. Phys. Rev. Lett. 55, 418-421 (1985)
Cox. “The Electronic Structure and Chemistry of Solids”. Oxford Science Publications (2005)
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 25
MaXb
X p-band
M dn+1/dn
M dn/dn-1
E
U
Δ
Directly related to Madelung potential and EN of anion X
Mott-Hubbard vs. charge transfer dominated character will alter potential
Zaanen, Sawatzky & Allen. Phys. Rev. Lett. 55, 418-421 (1985)
Cox. “The Electronic Structure and Chemistry of Solids”. Oxford Science Publications (2005)
Increases across the row of TMs from L to R
Notes: Hubbard assumes that the only important repulsion effects occur between two electrons on the same atom.

## Slide 26
MaXb
X p-band
M dn+1/dn
M dn/dn-1
E
U
Δ
Mott-Hubbard vs. charge transfer character
will alter electrode potential
X p-band
M dn+1/dn
M dn/dn-1
E
U
Δ
early TM compounds
M = Ti, V, . . .
late TM compounds
M = Co, Ni, Cu, . . .
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 27
MaXb
X p-band
M dn+1/dn
M dn/dn-1
U
EMF
Mott-Hubbard vs. charge transfer character
will alter electrode potential
X p-band
M dn+1/dn
M dn/dn-1
Δ
early TM compounds
M = Ti, V, . . .
late TM compounds
M = Co, Ni, Cu, . . .
Li+/Li0
Li+/Li0
EMF
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 28
For early TMs, we can consider the potential to be defined by the d-band redox couples
Adapted from Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
Li0TiS2
Li+/Li0
S p-band
Ti d4+/d3+
Ti d3+/d2+
EMF
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 29
For early TMs, we can consider the potential to be defined by the d-band redox couples
Adapted from Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
Li0TiS2
S p-band
Li0.5TiS2
EMF
EMF
We approximate the
d-band to be sufficiently narrow that a redox couple will have a singular energy
Li+/Li0
Ti d4+/d3+
Ti d3+/d2+
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 30
For early TMs, we can consider the potential to be defined by the d-band redox couples
Adapted from Goodenough & Kim. Chem. Mater. 22, 587-603 (2010).
Li0TiS2
S p-band
LiTiS2
LiTiS2
EMF
Li+/Li0
EMF
EMF
Ti d4+/d3+
Ti d3+/d2+
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 31
Structure also affects potential: LiMn2O4 has octahedral and tetrahedral Li sites
Thackeray, Jahnson, De Picciotto, Bruce & Goodenough. Mater. Res. Bull. 19, 435 (1984).
LixMn2O4
Li+/Li0
O p-band
Mn (tet-Li) d4+/d3+
Mn (oct-Li) d4+/d3+
tetrahedral
octahedral
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 32
Structure also affects potential: LiMn2O4 has octahedral and tetrahedral Li sites
Thackeray, Jahnson, De Picciotto, Bruce & Goodenough. Mater. Res. Bull. 19, 435 (1984).
LixMn2O4
Li+/Li0
O p-band
Mn (tet-Li) d4+/d3+
Mn (oct-Li) d4+/d3+
tetrahedral
octahedral
EMF
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 33
Structure also affects potential: LiMn2O4 has octahedral and tetrahedral Li sites
Thackeray, Jahnson, De Picciotto, Bruce & Goodenough. Mater. Res. Bull. 19, 435 (1984).
LixMn2O4
O p-band
Mn (tet-Li) d4+/d3+
Mn (oct-Li) d4+/d3+
tetrahedral
octahedral
EMF
Li+/Li0
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 34
We can think about electrode EMF by DOS
MaXb
M = transition metal
X = anion (O, S, F, N)
X p-band
M dn+1/dn
M dn/dn-1
E
Position and BW of M d-bands
ionization energy
EN of anion
coordination of M
Position and BW of anion p-band
EN of anion
Madelung potential
Charge transfer vs. Mott-Hubbard
Nature of M and X
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 35
We can tailor electrode potential
to suit a specific application
Specific energy = capacity × Voc
Specific power = Specific energy × time to charge
. . . but that is one small piece of battery performance
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 36
We can tailor electrode potential
to suit a specific application
Specific energy = capacity × Voc
Specific power = Specific energy × time to charge
. . . but that is one small piece of battery performance
And these other factors depend heavily on kinetics and structure.
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 37
We can think about electrode EMF by DOS
MaXb
M = transition metal
X = anion (O, S, F, N)
X p-band
M dn+1/dn
M dn/dn-1
E
Position and BW of M d-bands
ionization energy
EN of anion
coordination of M
Position and BW of anion p-band
EN of anion
Madelung potential
Charge transfer vs. Mott-Hubbard
Nature of M and X
Notes: The energy can correspond to the fermi energy in an itinerant-electron band, or based on the energy of a redox couple of a transition metal cation

## Slide 38
Hayner, Zhao & Kung. Annu .Rev. Chem. Biomolec. Eng. 3, 445–71 (2012).
A wide range of potentials can be achieved
Notes: Can see variation with TM, anion, oxidation state

## Slide 39
Power and energy are common metrics
for comparing energy storage technologies
Hayner, Zhao & Kung. Annu .Rev. Chem. Biomolec. Eng. 3, 445–71 (2012).
Notes: Going beyond the Eg of the electrolyte can result in decomposition of the electrolyte, which will add complexity to the analysis and understanding.
So – what kinds of things influence the energy/potential of each electrode?

## Slide 40
cycling
Commercial electrodes typically function through Li intercalation
xLi+ +xe-+ Li1-xCoO2
LiCoO2
Ex:

## Slide 41
Madelung potential
Correction factor to account for ionic interactions – electrostatic potential of oppositely charged ions
Vm = Am(z*e)/(4*pi*Epsilon0*r)