## Slide 1
Comparing magnetic SrMO3 perovskites M= 3d vs. 4d
Leo Lamontagne
MTRL 286G
6/2/2014

## Slide 2: 3d vs. 4d magnetism
http://www.doitpoms.ac.uk/tlplib/ferromagnetic/types.php
3d:
Smaller bandwidth leads to stoner instabilities
Stronger correlation between electrons
4d:
Greater orbital overlap gives more disperse bands
Spin orbit coupling can play a role

## Slide 3: The perovskite structure distorts based on cation size
eg
t2g

## Slide 4: Spin ordering in magnetic perovskites
http://folk.uio.no/ravi/activity/ordering/spinfig.html

## Slide 5: Magnetism varies widely even among neighbors in PT
Magnetism present
Relations to DOS and structure

## Slide 6: SrCrO3 and SrMoO3
Zhu, Z.L, Gu, J.H., Jia, Y., Hu, X., Physica B, 407 (2012) p1990-1994
Both cubic, Pm-3m
SrMoO3 undergoes transition to tetragonal (I4/mcm) to orthorhombic (Imma).
SrCrO3, is cubic until 40-50K then tetragonal, P4/mmm

## Slide 7: SrCrO3 is AFM in the tetragonal phase
San-Martin, L.O., Williams, A.J., Rodgers, J., Attfield, J.P.,
Heymann, G., Huppertz, H., PRL, 99 (2007) 255701
Tetragonal phase made under high pressure shows AFM transition in SrCrO3
Cubic phases of both SrMoO3 and SrCrO3 are paramagnetic
Notes: C-type Antiferromagnet

## Slide 8: SrMnO3 crystallizes in a hexagonal structure
Sodena, R., Ravindran, P., Stolen, S., Grande, T., Hanfland, M. Phys Rev B, 74 (2006) 144102
G-type antiferromagnet with TN=280K in
At 750K, cubic with TN=250K
Oxygen stoichiometry can vary TN

## Slide 9: 4d analog SrTcO3 has extremely high TN
Rodriguez, E., Poineau, F., Llobet, A., Kennedy, B.J., Avdeev, M., Thorogood, G.J.,
Carter, M.L., Seshadri, R., Singh, D.J., Cheetham, A.K., PRL 106 (2011) 067201
Orthorhombic, Pnma
TN=750oC

## Slide 10: High TN is due to several factors
Mravlje, J. Aichhorn, M., Georges, A. PRL 108 (2012) 197202
High Tc-O bond covalency
Large band width
Half filled t2g and close to locaI-itinerant electrons

## Slide 11: SrFeO3 is a cubic AFM down to 4K
Takeda, T., Yamaguchi, Y., Watanabe, H. J. Phys. Soc. Jpn., 33 (1972) 967
Fe4+ is high spin with localized t2g electrons and itinerant eg so no Jahn Teller distortion is observed
Antiferromagnetic with helical spin structure
eg
t2g

## Slide 12: SrRuO3 is ferromagnetic
Barton, P.T., Seshadri, R., Rosseinsky, M. Phys. Rev. B., 83 (2011) 064417
eg
t2g
Orthorhombic, Pnma, at room temperature
Mixed itinerant/local electron behavior
Rhodes-Wohlfarth ratio probes degree of itinerant behavior

## Slide 13: Structural distortions can weaken FM
Park, J.C., Kim, D., Lee, C.S., Byeon, S.H., Bull Korean Chem Soc, 24 (2003) 650

## Slide 14: Conclusions
Type of magnetism and transition temperature can vary widely from 3d to 4d
Broad bands in 4d metals can significantly effect type of magnetism
M-O covalency can change transition temperature
Structural distortions can weaken magnetism