## Slide 1
Class 04. Correlations and the Hubbard model: LaMnO3
Jahn-Teller distorted orthorhombic perovskite (space group Pnma)

## Slide 2
Class 04. Correlations and the Hubbard model: LaMnO3
Structure and magnetism do not explain the insulating behavior.

## Slide 3
Class 04. Correlations and the Hubbard model: LaMnO3
Electrical resistivity behavior in La1–xSrxMnO3
Anane, Dupast, Dang, Renard, Veillet, de Leon Guevare, Millot, Pinsard, Revcolevschi, J. Phys.: Condens. Matter 7 (1995) 7015-7021.

## Slide 4
Class 04. Correlations and the Hubbard model: NiO
NiO displays the color of isolated Ni2+ in solution, with similar spectra.

## Slide 5
Class 04. Correlations and the Hubbard model: NiO
NiO displays the color of isolated Ni2+ in solution, with similar spectra.
From the Cox text, page 151

## Slide 6
Class 04. Correlations and the Hubbard model: NiO, spectroscopic studies

## Slide 7
Class 04. Correlations and the Hubbard model: The idea of Mott
Consider a chain of orbitals, each with one electron. To hop an electron, an orbital has to be ionized at cost I, which is compensated a little by the electron affinity A.
U = I – A
For H atoms, I = 13.6 eV and A = 0.8 eV, meaning U = 12.8 eV. However, this does not account for some screening (due to the dielectric not being vacuum).
From the Cox text, page 135

## Slide 8
Class 04. Correlations and the Hubbard model: The Hamiltonian
hopping or tight-binding (LCAO) part
double-occupancy cost or on-site repulsion

## Slide 9
Class 04. Correlations and the Hubbard model: The Hamiltonian
From the Cox text, page 137
As the bandwidth is increased, (or as the atoms approach closer) the gap can close.

## Slide 10
Class 04. Correlations and the Hubbard model: The Hamiltonian
From the Cox text, page 149
Doping of holes (removal of electrons) as in (b) makes hopping much easier, with the on-site repulsion having been removed.