## Slide 1
Class 05. The Hubard model and magnetism
On the insulating side of the M–I transition, magnetism of some sort (usually antiferromagnetism) manifests.

## Slide 2
Class 05. The Hubard model and magnetism
In the limit that U >> t, the Hubbard model:
Can be reduced to the Heisenberg Hamiltonian:
where

## Slide 3
Class 05. The Hubard model and magnetism [will return to these !]
The example of LnNiO3, Ln = La, Pr, Nd, Sm:
Torrance, Lacorre, Nazzal, Ansaldo, Niedermayer, Phys. Rev. B. 45 (1992) 8209–8212.

## Slide 4
Class 05. The Zaanen-Sawatzky-Allen phase diagram
The position of transition metal d-states vs. anion p states:
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.

## Slide 5
Class 05. The Zaanen-Sawatzky-Allen phase diagram
The actual diagram. Note that T is what we have been calling W, and W is proportional to t in the Hubbard Model.
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.

## Slide 6
Class 05. The Zaanen-Sawatzky-Allen phase diagram
A simplified view: In the language of ZSA:
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.
lower Hubbard
upper Hubbard
U
Mott-Hubbard insulators:
lower Hubbard
upper Hubbard
D
Charge-transfer insulators:
anion p states
anion p states

## Slide 7
Class 05. The Zaanen-Sawatzky-Allen phase diagram
Examples of Mott-Hubbard: V2O3, Ti2O3, Cr2O3 and most halides. Early transition metals, and lower oxidation states. Interestingly, these do display T-dependent M–I transitions.
Examples of Charge-transfer: CuO, NiCl2, NiS, etc. Later transition metals and higher oxidation states. CuO and NiCl2 are always insulating.
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.

## Slide 8
Class 05. The Zaanen-Sawatzky-Allen phase diagram. Periodic trends
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.

## Slide 9
Class 05. The Zaanen-Sawatzky-Allen phase diagram and perovskites
Optical studies of band gaps: Distinguishing d–d and p–d character:
Arima, Tokura, Torrance, Phys. Rev. B. 48 (1993) 17006–17009.

## Slide 10
Class 05. The Zaanen-Sawatzky-Allen phase diagram and perovskites

## Slide 11
Class 05. The Zaanen-Sawatzky-Allen phase diagram and batteries
The transition metal d and anion p levels manifest in Li-battery electrochemistry.
Hayner, Zhao, Kung, Annu. Rev. Chem. Biomolec. Eng. 3 (2012) 445–471.

## Slide 12
Class 05. The Zaanen-Sawatzky-Allen phase diagram and redox competition
Ideas of Goodenough, Rouxel etc.
M4+
M2+

## Slide 13
Class 05. The Zaanen-Sawatzky-Allen phase diagram and redox competition