## Slide 1
Class 12, Experimental techniques: Resistivity
Ultrathin Bi films. “The onset of superconductivity in homogeneous ultrathin films is found to occur when their normal state
sheet resistance falls below a value close to h/(4e2), the quantum resistance for pairs. The data further
suggest that in the T = 0 limit such films are either superconducting or insulating.”
Haviland, Liu, Goldman, Phys. Rev. Lett. 62 (1989) 2180–2183.

## Slide 2
Resistivity of a semiconductor:
Resistivity of a system with a mobility edge:
Variable range hopping or VRH (d is the dimensionality):
for a 3D system.
Class 12, Experimental techniques: Resistivity

## Slide 3
Epstein, Lee, Progodin, Synth. Met. 117 (2001) 9–13.
Conducting polymers (quasi–1D): Polyaniline and polypyrrole.
Class 12, Experimental techniques: Resistivity

## Slide 4
Khondaker, Shlimak, Nicholls, Pepper, Ritchie, Phys. Rev. B. 59 (1999) 4580–4583.
A 2D system: d-doped GaAs/AlGaAs heterostructures.
Class 12, Experimental techniques: Resistivity

## Slide 5
Khondaker, Shlimak, Nicholls, Pepper, Ritchie, Phys. Rev. B. 59 (1999) 4580–4583.
A 2D system: d-doped GaAs/AlGaAs heterostructures.
“The inset shows the same data plotted as ln W versus ln T; the slope gives the exponent p.
Around 1 K there is a change of slope of ln W as p changes from 0.55±0.05 to 0.34±0.03.”
This change to the slope close to 1 /2 signifies Efros-Shklovskii hopping due to Coulomb correlations:
Class 12, Experimental techniques: Resistivity

## Slide 6
Zhou, Marshall, Goodenough, Mass enhancement versus Stoner enhancement in strongly correlated metallic perovskites: LaNiO3 and LaCuO3, Phys. Rev. B. 89 (2014) 245138(1–8).
LaNiO3 and LaCuO3 prepared under pressure.
Class 12, Experimental techniques: Seebeck, heat capacity, etc.

## Slide 7
Zhou, Marshall, Goodenough, Mass enhancement versus Stoner enhancement in strongly correlated metallic perovskites: LaNiO3 and LaCuO3, Phys. Rev. B. 89 (2014) 245138(1–8).
LaNiO3 and LaCuO3 prepared under pressure.
Class 12, Experimental techniques: Seebeck, heat capacity, etc.

## Slide 8
Kondo et al., LiV2O4: A heavy fermion transition metal oxide, Phys. Rev. Lett. 79 (1997) 3729–3732.
LiV2O4: Heavy fermions !
g = 0.42 J/mol-K2 is exceptionally large for a transition metal compound.
The Wilson ratio is 1.7
Class 12, Experimental techniques: Seebeck, heat capacity, etc.

## Slide 9
From Imada, Fujimori, Tokura, Rev. Mod. Phys.
The pyrite system: NiS2–xSex
Class 12, Experimental techniques: Photoemission

## Slide 10
From Imada, Fujimori, Tokura, Rev. Mod. Phys.
Angle-resolved photoemission of NiS1.5Se0.5
Class 12, Experimental techniques: Photoemission

## Slide 11
Lanzara, Saini, Brunelli, Natali, Bianconi, Radaelli, Cheong, Crossover from Large to Small Polarons across the Metal-Insulator Transition in Manganites, Phys. Rev. Lett. 81 (1998) 878–881.
La0.75Ca0.25MnO3 studied by x-ray absorption (EXAFS) across the transition.
Class 12, Experimental techniques: Probing polarons with XAS

## Slide 12
Berggold, Kriener, Zobel, Reichl, Reuther, Müller, Freimuth, Lorenz, Phys. Rev. B 72 (2005) 155116(1–7).
La1–xSrxCoO3:
Class 12, Experimental techniques: Probing polarons with thermal transport