## Slide 1: Iridates
Bill Flaherty
Materials 286K, UCSB
Dec. 8th, 2014

## Slide 2: 5d transition metals: uninteresting?
“The properties of the 4d and 5d compounds tend to be less exotic” – Mattheiss, 1976
3d transition metal oxides: localized states
  Strong correlations
  Narrow bands, large U/W
4d, 5d: spatially extended states
  Wide bandwidth
  Low on-site repulsion, smaller U/W
  Predicted to be metallic, ferromagnetic

## Slide 3: Discovery of “MORE EXOTIC” 4d, 5d TMOs
  Sr2IrO4 - M. K. Crawford et al., Phys. Rev. B 49, 9198 (1994).
  Sr2IrO4, Sr2RuO4 - R. J. Cava et al., Phys. Rev. B 49, 11 890 (1994)
  Ca2-xSrxRuO4 - S. Nakatsuji and Y. Maeno, Phys. Rev. Lett. 84, 2666 (2000)
  Cd2Os2O7 - D. Mandrus et al., Phys. Rev. B 63, 195104 (2001).
  Y, Ca, Sr, Bi Ruthenates - J. S. Lee et al., Phys. Rev. B 64, 245107 (2001).

## Slide 4: Sr-214 Band structure
Sr2(2+)Ir(4+)O4
Ir(4+): 5d5 system

## Slide 5: Sr-214: correct Band structure
Spin-Orbit Coupling (SOC)
t2g states → l = 1 states
Strong SOC:
t2g splits into Jeff = 3/2 and 1/2
Narrow Jeff = ½ band due to hopping integrals
Novel Jeff = 1/2 Mott State Induced by Relativistic Spin-Orbit Coupling in Sr2IrO4
B. J. Kim et al., Phys. Rev. Lett 101, 076402 (2008)

## Slide 6: Observation of u + SOC
ARPES, Optical Conductivity, XAS experiments
DFT calculations (LDA, LDA + U)
Novel Jeff = 1/2 Mott State Induced by Relativistic Spin-Orbit Coupling in Sr2IrO4
B. J. Kim et al., Phys. Rev. Lett 101, 076402 (2008)

## Slide 7: Resonant x-ray studies
Resonant X-ray Spectroscopy
  Contains information from quantum interference
  of different scattering paths
Phase-Sensitive Observation of a Spin-Orbital Mott State in Sr2IrO4
B. J. Kim et al., Science 323, 1329 (2009)

## Slide 8: Phase-sensitive measurements
Jeff = ½ states – linear combinations of xy, yz, zx that differ in phase
No phase difference for simple t2g states (real wave fns.)
Scattering amplitudes depend on phase differences between states
→ Test Jeff = ½ model vs. S = ½
Phase-Sensitive Observation of a Spin-Orbital Mott State in Sr2IrO4
B. J. Kim et al., Science 323, 1329 (2009)

## Slide 9: Results
Phase-Sensitive Observation of a Spin-Orbital Mott State in Sr2IrO4
B. J. Kim et al., Science 323, 1329 (2009)

## Slide 10: Tuning the I.-m.T. with Structure
How can we tune U/W?
Bandwidth depends on number of Ir nearest neighbors
Grow different Ruddelsden-Popper phases to change W and tune U/W

## Slide 11: Ruddelsden-Popper phases
Srn+1IrnO3n+1
n = 1 Sr2IrO4
four nearest neighbors
n = 2 Sr3Ir2O7
five nearest neighbors
n → infinity SrIrO3
(Perovskite on MgO substrate)
six nearest neighbors
Figure from D. A. Zocco et al., J. Phys.: Condens. Matter 26, 255603 (2014)

## Slide 12: Results – Lda + U
Insulating Sr2IrO4
Barely Insulating Sr3Ir2O7
Correlated Metal SrIrO3
U = 2 eV
U typically much larger for a Mott Ins, 4-7 eV
S. J. Moon et al., Phys. Rev. Lett. 101, 226402 (2008)

## Slide 13: results
Optical Conductivity
S. J. Moon et al., Phys. Rev. Lett. 101, 226402 (2008)

## Slide 14: Topological Mott insulators
SOC scales by atomic number as Z4
Hg and Bi – strong SOC, weak correlation (s- and p-states)

## Slide 15: Topological insulators
Bulk is insulating
Conducting surface states
Robust against defects
  topologically protected states
Potential uses for quantum computing
  Unusual particle statistics – Dirac fermions (SmB6 – 2014)
  Delocalized states resistant against decoherence

## Slide 16: Pyrochlore Iridates
A2(3+)Ir2(4+)O7
Spinons, quantum criticality
TBI – Topological Band Ins
GMI – Gapless Mott Ins
TMI – Topological Mott Ins
  Charge-spin separation
  Spinons – gapless spin excitations
  Insulating surface states