## Slide 2
M—I Transition In Rare-Earth Nickelates And The Impact Of Structural Distortions
Outline:
LaNiO3: The basics
Tuning the Metal-Insulator Transition
  Structural distortions
  Oxygen deficiency
  Dimensionality

## Slide 3
LaNiO3
Remember me?

## Slide 4
LaNiO3
Remember me?

## Slide 5
Gou et al., Phys. Rev. B 84 (2011) 144101.
LaNiO3: An Introduction
Paramagnetic
Correlated metal

## Slide 6
LaNiO3: An Introduction
Paramagnetic
Correlated metal
Sanchez et al., Phys. Rev. B 54 (1996) 16574-16578.
Sreedhar et al., Phys. Rev. B 46 (1992) 6382-6386.

## Slide 7
Rare earth size allows tuning structural distortions
Varying A-site radius: LnNiO3
Medarde et al., J. Phys. Condensed Matter 9 (1997) 1679.
Problem: Hard to prepare…

## Slide 8
Varying A-site radius: LnNiO3
Structural distortions dictate the M–I transition of LnNiO3
Torrance et al. Phys. Rev. B. 45 (1992) 8209–8212.

## Slide 9
Measuring structural distortions with neutron diffraction
Varying A-site radius: LnNiO3
Garcia-Munoz et al., Phys. Rev. B 46 (1992) 4414-4425.

## Slide 10
Staub et al., Phys. Rev. Lett. 88 (2002) 126402.
Charge ordering: 2 Ni3+ -> Ni(3+δ)+ + Ni(3-δ’)+
Varying A-site radius: LnNiO3
For NdNiO3, δ+δ’ = 0.45
Smaller than bond-valence sum (0.6)

## Slide 11
Obradors et al. Phys. Rev. B 47 (1993) 12353.
Zhou et al., Phys. Rev. B 61 (2000) 4401-4404.
Pressure effects – alters oxygen vibration frequency
Varying A-site radius: LnNiO3
NdNiO3
PrNiO3
LaNiO3
Sm0.5Nd0.5NiO3

## Slide 12
Medarde et al., Phys. Rev. Lett. 80 (1998) 2397–2400.
Lattice dynamics (i.e. electron-lattice coupling) plays an important role
Varying A-site radius: LnNiO3

## Slide 13
M—I Transition In Rare-Earth Nickelates And The Impact Of Structural Distortions
Outline:
LaNiO3: The basics
Tuning the Metal-Insulator Transition
  Structural distortions
  Oxygen deficiency
  Dimensionality

## Slide 14
Sanchez et al., Phys. Rev. B 54 (1996) 16574-16578.
Qiao and Bi, Europhysics Lett. 93 (2011) 57002.
Oxygen Deficiency: LaNiO3-δ
Metal-Insulator transition near δ = 0.25
LaNiO2.84
LaNiO2.64

## Slide 15
Sanchez et al., Phys. Rev. B 96 (1996) 16574-16578.
Qiao and Bi, Europhysics Lett. 93 (2011) 57002.
Oxygen Deficiency: LaNiO3-δ
rNi3+ = 0.60 nm
rNi2+ = 0.69 nm
LaNiO2.75
LaNiO2.5

## Slide 16
M—I Transition In Rare-Earth Nickelates And The Impact Of Structural Distortions
Outline:
LaNiO3: The basics
Tuning the Metal-Insulator Transition
  Structural distortions
  Oxygen deficiency
  Dimensionality

## Slide 17
Scherwitzl et al., Phys. Rev. Lett. 106 (2011) 246403.
Son et al., Appl. Phys. Lett. 96 (2010) 062114.
Ioffe-Regel limit:
kF l = h/e2 = 25kΩ/sq --> 1
Rs Rs
Tuning Dimensionality: Thin LaNiO3
LSAT
DyScO3
LaAlO3
SrTiO3

## Slide 18
Scherwitzl et al., Appl. Phys. Lett. 95 (2009) 222114.
Tuning TMI with gate bias
Tuning Dimensionality: Thin LaNiO3

## Slide 19
M—I Transition In Rare-Earth Nickelates And The Impact Of Structural Distortions
Summary:
Multiple methods to tune across metal-insulator transition in LnNiO3
  Distorting Ni – O – Ni bond angle
    Rare earth cation radius
    Pressure
  Oxygen deficiency (Ni oxidation state)
  Dimensionality

## Slide 20
Citation
Text
Title