## Slide 1
NMR Studies of Metal-Insulator Transitions
Leo Lamontagne
MATRL286K
December 10th, 2014

## Slide 2: Intro to Nuclear Magnetic Resonance
Element specific technique utilizing nuclear spins of atoms
Nuclear spins are aligned in a magnetic field and pulsed with a radio frequency causing spins to precess.
Local environments around the nucleus can change the effective magnetic field resulting in slight shifts of the precession frequency
ω0= γ⋅B0

## Slide 3: Nuclear spins separate in energy in a magnetic field
Energy separation between aligned and anti-aligned states is in the MHz range. The decay of excited nuclei is measured
http://www.chem.ucalgary.ca/courses/350/Carey5th/Ch13/ch13-nmr-1b.html

## Slide 4
http://www.bruker-nmr.de/guide/eNMR/chem/NMRnuclei.html

## Slide 5: The Knight Shift
Shift from Larmor frequency in metals due to the polarization of the conduction electrons
W. D. Knight, Phys. Rev. 76 (1949) 1259-1260

## Slide 6
Shift of the Cu peak in Cu metal as compared to CuCl
“shift may be due to the paramagnetic effect of the conduction electrons in the vicinities of the metal nuclei”
W. D. Knight, Phys. Rev. 76 (1949) 1259-1260

## Slide 7: Simple Schematic Representation
http://www.fis.unipr.it/~derenzi/dispense/pmwiki.php?n=NMR.Knight
Blue line is larmor frequency of nucleus
Red peak is Knight shifted to higher frequency
% difference frequently reported

## Slide 8: MIT in expanded mercury
W. W. Warren, F. Hensel, Phys. Rev. B. 26 (1982) 5980-5982
At low densities, the knight shift drops sharply corresponding with onset of semiconducting behavior

## Slide 9
W. W. Warren, F. Hensel, Phys. Rev. B. 26 (1982) 5980-5982
Density of MIT in liquid determined through NMR, corresponds with onset of “plasma transition” in gas phase

## Slide 10: LixCoO2 gets more conductive upon Li deintercalation
M. Menetrier, I. Saadoune, S. Levasseur, C. Delmas, J. Mater. Chem. 9 (1999) 1135-1140
Conductivity increases by about 6 orders of magnitude and for x<0.70
Metallic behavior is seen at high temperature
Phase separation proposed from shoulders in XRD pattern

## Slide 11: 2 phase nature is confirmed by NMR
Below x=0.94 two phases arise,
Li0.94CoO2 and Li0.75CoO2
The peak of the second phase is knight shifted
Shift increases with increasing hole concentration
M. Menetrier, I. Saadoune, S. Levasseur, C. Delmas, J. Mater. Chem. 9 (1999) 1135-1140

## Slide 12: NMR shows spin state transitions in RCoO3
M. Itoh, J. Hasimoto, S. Yamaguchi, Y. Tokura, Physica B 281 (2000) 510-511
LaCoO3 transitions from LS to IS around 100 K, and is a metal above 500 K
NMR shows similar MIT in other rare-earths without IS transition

## Slide 13: NMR in V2O3 confirms no local moments in metallic state
A. C. Gossard, D. B. McWhan, J. P. Remeika, Phys. Rev. B. 2 (1970) 3762-3768
V2O3 is AFI at low temperatures
Can be driven metallic with pressure
Presence of signal indicates MIT is “accompanied by transition from localized magnetic moment behavior to band magnetism”

## Slide 14: Sharp change in Knight Shift indicates MIT
T. Waki, H. Kato, M. Kato, K. Yoshimura, J. Phys. Soc. Jpn. 73 (2004) 275-279
Bi1.6V8O16 is metallic at all temperatures
Bi1.77V8O16 becomes insulating below ~80 K

## Slide 15: Korringa relationship also demonstrates metallic behavior
T. Waki, H. Kato, M. Kato, K. Yoshimura, J. Phys. Soc. Jpn. 73 (2004) 275-279
T1 spin-lattice relaxation time is proportional to temperature for metals
Deviations can inform electron correlation or spin frustration

## Slide 16: 23Na NMR confirms formation of insulating phase with doping
M. Ricco, G. Fumera, T. Shiroka, O. Ligabue, C. Bucci, F. Bolzoni, Phys. Rev. B. 68 (2003) 035102
(NH3)xNaK2C60 is superconducting for x<1
Increasing ammonia further results in formation of insulating phase

## Slide 17: Korringa relation illustrates transition
M. Ricco, G. Fumera, T. Shiroka, O. Ligabue, C. Bucci, F. Bolzoni, Phys. Rev. B. 68 (2003) 035102
Thermally activated nuclear relaxations for the insulating sample
Potential charge disproportions from C60 anions

## Slide 18: Conclusions
NMR is an element specific technique which probes the local environment
The Knight Shift results from the polarization of the conduction electrons in metals
Metal-insulator transitions can be observed through NMR via the Knight Shift and relaxation times in a variety of systems