## Slide 1
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This figure, from page 137 of Zallen, describes the problem in a 2D square mesh.
At some precise critical number of random snips, current flow stops.
This is an example of bond percolation as opposed to site percolation.

## Slide 2
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This figure is from page 143 of Zallen.
This shows site percolation on a square lattice, with different site filling fractions p. For p = 0.75 in (c), the cluster formed by connecting neighboring atoms spans the whole lattice, and a percolation path is created.

## Slide 3
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This figure is from page 146 of Zallen.
Computer simulations on a large square lattice; sav(p) is the average cluster size, and P(p) is the percolation probability.

## Slide 4
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This table is from page 148 of Zallen.
Where is percolation applicable?

## Slide 5
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This table is from page 168 of Zallen.
Different lattices:

## Slide 6
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This table is from page 168 of Zallen.
Page 170 of Zallen.

## Slide 7
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This figure is from page 187 of Zallen.
There is a simple scaling in 3D, between both the site and bond percolation thresholds, with the packing fraction and coordination number, and the percolation thresholds.

## Slide 8
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This figure is from page 243 of Zallen.
The non-metal to metal transition on Si:P.
4pc is the dielectric sucseptibility.
Note the similarity with percolation (the third slide in this set of slides).
Measurements by Rosenbaum and others at 10 mK.

## Slide 9
Percolation etc. [Closely following the text by R. Zallen]
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This figure is from page 244 of Zallen.
Showing the percolation of hydrogenic wave-functions around the phosphorus donor atoms (much larger than the interatomic spacing).
Since P substitution is random, this is a problem of percolation in a random close packing.

## Slide 10
Percolation ?
La1–xSrxCoO3
Wu, Leighton, Phys. Rev. B 67 (2003) 174408.

## Slide 11
Percolation ?
La1–xSrxCoO3
Wu, Leighton, Phys. Rev. B 67 (2003) 174408.

## Slide 12
Anderson localization and the mobility edge
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This figure is from pages 229 and 232 of Zallen.
The Mott and Anderson transitions represented graphically in 1D.

## Slide 13
Anderson localization and the mobility edge
R. Zallen, The Physics of Amorphous Solids, Wiley-VCH, 2004.
This figure is from page 235 of Zallen.
The notion of the mobility edge.

## Slide 14
Correlations and the Hubbard model: LaMnO3
Jahn-Teller distorted orthorhombic perovskite (space group Pnma)

## Slide 15
Correlations and the Hubbard model: LaMnO3
Structure and magnetism do not explain the insulating behavior.

## Slide 16
Correlations and the Hubbard model: LaMnO3
Electrical resistivity behavior in La1–xSrxMnO3
Anane, Dupast, Dang, Renard, Veillet, de Leon Guevare, Millot, Pinsard, Revcolevschi, J. Phys.: Condens. Matter 7 (1995) 7015-7021.

## Slide 17
Correlations and the Hubbard model: NiO
NiO displays the color of isolated Ni2+ in solution, with similar spectra.

## Slide 18
Correlations and the Hubbard model: NiO
NiO displays the color of isolated Ni2+ in solution, with similar spectra.
From the Cox text, page 151

## Slide 19
Correlations and the Hubbard model: NiO, spectroscopic studies

## Slide 20
Correlations and the Hubbard model: The idea of Mott
Consider a chain of orbitals, each with one electron. To hop an electron, an orbital has to be ionized at cost I, which is compensated a little by the electron affinity A.
U = I – A
For H atoms, I = 13.6 eV and A = 0.8 eV, meaning U = 12.8 eV. However, this does not account for some screening (due to the dielectric not being vacuum).
From the Cox text, page 135

## Slide 21
Correlations and the Hubbard model: The Hamiltonian
hopping or tight-binding (LCAO) part
double-occupancy cost or on-site repulsion

## Slide 22
Correlations and the Hubbard model: The Hamiltonian
From the Cox text, page 137
As the bandwidth is increased, (or as the atoms approach closer) the gap can close.

## Slide 23
Correlations and the Hubbard model: The Hamiltonian
From the Cox text, page 149
Doping of holes (removal of electrons) as in (b) makes hopping much easier, with the on-site repulsion having been removed.

## Slide 24
The Hubard model and magnetism
On the insulating side of the M–I transition, magnetism of some sort (usually antiferromagnetism) manifests.

## Slide 25
The Hubard model and magnetism
In the limit that U >> t, the Hubbard model:
Can be reduced to the Heisenberg Hamiltonian:
where

## Slide 26
The Hubard model and magnetism [will return to these !]
The example of LnNiO3, Ln = La, Pr, Nd, Sm:
Torrance, Lacorre, Nazzal, Ansaldo, Niedermayer, Phys. Rev. B. 45 (1992) 8209–8212.

## Slide 27
The Zaanen-Sawatzky-Allen phase diagram
The position of transition metal d-states vs. anion p states:
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.

## Slide 28
The Zaanen-Sawatzky-Allen phase diagram
The actual diagram. Note that T is what we have been calling W, and W is proportional to t in the Hubbard Model.
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.

## Slide 29
The Zaanen-Sawatzky-Allen phase diagram
A simplified view: In the language of ZSA:
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.
lower Hubbard
upper Hubbard
U
Mott-Hubbard insulators:
lower Hubbard
upper Hubbard
D
Charge-transfer insulators:
anion p states
anion p states

## Slide 30
The Zaanen-Sawatzky-Allen phase diagram
Examples of Mott-Hubbard: V2O3, Ti2O3, Cr2O3 and most halides. Early transition metals, and lower oxidation states. Interestingly, these do display T-dependent M–I transitions.
Examples of Charge-transfer: CuO, NiCl2, NiS, etc. Later transition metals and higher oxidation states. CuO and NiCl2 are always insulating.
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.

## Slide 31
The Zaanen-Sawatzky-Allen phase diagram. Periodic trends
Zaanen, Sawatzky, Allen, Phys. Rev. Lett. 55 (1985) 418–421.

## Slide 32
The Zaanen-Sawatzky-Allen phase diagram and perovskites
Optical studies of band gaps: Distinguishing d–d and p–d character:
Arima, Tokura, Torrance, Phys. Rev. B. 48 (1993) 17006–17009.

## Slide 33
The Zaanen-Sawatzky-Allen phase diagram and perovskites

## Slide 34
The Zaanen-Sawatzky-Allen phase diagram and batteries
The transition metal d and anion p levels manifest in Li-battery electrochemistry.
Hayner, Zhao, Kung, Annu. Rev. Chem. Biomolec. Eng. 3 (2012) 445–471.

## Slide 35
The Zaanen-Sawatzky-Allen phase diagram and redox competition
Ideas of Goodenough, Rouxel etc.
M4+
M2+

## Slide 36
The Zaanen-Sawatzky-Allen phase diagram and redox competition