## Slide 1
Oxide crystal structures: The basics
Ram Seshadri
Materials Department and Department of Chemistry & Biochemistry
Materials Research Laboratory, University of California, Santa Barbara CA 93106 USA
seshadri@mrl.ucsb.edu
Materials 286G, Spring 2020

## Slide 2
en.wikipedia.org:
“Helen Dick Megaw (1 June 1907 – 26 February 2002) was an Irish crystallographer who was a pioneer in X-ray crystallography. She made measurements of the cell dimensions of ice and established the Perovskite crystal structure.”

## Slide 3
This lecture
Brief description of oxide crystal structures
Ionic radii and Pauling’s rules
Electrostatic valence
Bond valence, and bond valence sums
Connectivity and bandwidth
First rule: the radius ratio rule
Second rule: the electrostatic valence rule
Third rule: sharing of polyhedron corners, edges and faces
Fourth rule: crystals containing different cations
Fifth rule: the rule of parsimony

## Slide 4
Ionic radii and Pauling’s first rule (the radius ratio rule)
In brief: The cation-anion distance is the sum of cation and anion radii, and the number of anions around a cation (the coordination number) is a function of the radius ratio. Exemplified by AO2 compounds below. MRR below is the mimimum radius ratio.
Pauling, The Nature of the Chemical Bond, 3rd Edn., Cornell University Press, Ithaca 1960

## Slide 5
Crystal structures of simple oxides [containing a single cation site]

## Slide 6
Crystal structures of simple oxides [containing a single cation site]
N.B.: CoO is simple, Co3O4 is not. ZnCo2O4 is certainly not !
Co3O4 and ZnCo2O4 are complex oxides.
Graphs of connectivity in crystals: Atoms are nodes and edges (the lines that connect nodes) indicate short (near-neighbor) distances.
CO2: The molecular structure is O=C=O. The graph is:
Each C connected to 2 O, each O connected to a 1 C
OsO4: The structure comprises isolated tetrahedra (molecular). The graph is below:
Each Os connected to 4 O and each O to 1 Os

## Slide 7
Crystal structures of simple oxides of monovalent ions: A2O
Cu2O
Na2O (anti-fluorite)
Linear coordination is unusual. Found usually in Cu+ and Ag+.
4-coordination for Na+ and 8-coordination for O2– are unusual.

## Slide 8
Crystal structures of simple oxides of divalent ions: AO
ZnO (wurtzite), sp3
PbO (litharge), lone pairs
Pb2+ is [Xe]4f145d106s26p0
MgO (rock-salt)
Ubiquitous for AO oxides including transition metals (distorted for CuO and NbO).
Insulators, metals (TiO), magnetic, …

## Slide 9
Crystal structures of simple oxides. Al2O3 as an example of a sesquioxide
a-Al2O3 (corundum)
Also the structure of Cr2O3 and Fe2O3.
Ga2O3 does funny things.
In2O3 is different (bixbyite).

## Slide 10
B2O3 (chiral, P3121)
B2O3 (hugely important for glass industry).
NB: This structure is not in scale with the others.

## Slide 11
Crystal structures of simple oxides of tetravalent ions: AO2
TiO2 (rutile)
CeO2 (fluorite)
TiO2 also crystallizes as anatase and brookite.
SiO2 takes on this structure, and can be quenched to it, (stishovite) under pressure.
Also the structure of ThO2, and of ZrO2 and HfO2 at elevated temperatures.
Ordered variants abound.
The radius ratio rule at play:
CO2 Linear
SiO2 Tetrahedral
TiO2 Octahedral
HfO2 7-coordinate
CeO2 Cubic

## Slide 12
Oxides versus sulfides: TiS2
1T–TiS2
van der Waals gap (unlikely in oxides or fluorides, but occurs frequently in hydroxides)
This is the CdI2 structure.

## Slide 13
Crystal structures of an oxide with an octavalent ion: OsO4
OsO4

## Slide 14
Pauling’s second rule: The electrostatic valence rule
In brief: Charges going out from cations should balance anions and vice-versa
Pauling, The Nature of the Chemical Bond, 3rd Edn., Cornell University Press, Ithaca 1960
+1/2
+8/4
+3/6
electrostatic bond strength or valence
s = charge on cation/coordination number
Why is OsO4 a molecule? Radius ratio + electrostatic valence

## Slide 15
Electrostatic valence and bond valence
Pauling, and later Brown and Shannon, noted that the Pauling bond strength (the electrostatic valence) correlates very well with distance for many oxides: Short bonds (distances) correspond to strong bonds and vice-versa
Brown, Shannon, Empirical bond-strength-bond-length curves for oxides, Acta Cryst. A 29 (1973) 266–281

## Slide 16
Electrostatic valence and bond valence
The modern bond valence relationship:
Where s is the strength of the bond, R is the cation to anion distance, and R0 and B (≈ 0.37 Å) are parametrized for the specific ion pair.
When all s are calculated: valence of the ion
Brown, Shannon, Empirical bond-strength-bond-length curves for oxides, Acta Cryst. A 29 (1973) 266–281.
For Mn2+–O2–, R0 = 1.790 Å, B = 0.37 Å.
This means R = 2.20 Å.
experiment: 2.22 Å
s = +2/6

## Slide 17
Electrostatic valence and bond valence: Parameters for Mn
Mn 2 O -2 1.790 0.37 a
Mn 2 O -2 1.765 0.37 j
Mn 2 S -2 2.22 0.37 e
Mn 2 F -1 1.698 0.37 a
Mn 2 Cl -1 2.133 0.37 a
Mn 2 Br -1 2.34 0.37 e
Mn 2 I -2 2.52 0.37 e
Mn 2 N -3 1.849 0.37 j
Mn 2 N -3 1.65 0.35 e
Mn 3 O -2 1.760 0.37 a
Mn 3 O -2 1.732 0.37 j
Mn 3 F -1 1.66 0.37 b
Mn 3 Cl -1 2.14 0.37 b
Mn 3 N -3 1.837 0.37 j
Mn 4 O -2 1.753 0.37 a
Mn 4 O -2 1.750 0.37 j
Mn 4 F -1 1.71 0.37 b
Mn 4 F -1 1.63 0.37 e
Mn 4 Cl -1 2.13 0.37 b
Mn 4 N -3 1.822 0.37 j
Mn 6 O -2 1.79 0.37 e
Mn 7 O -2 1.827 0.37 e
Mn 7 O -2 1.79 0.37 b
Mn 7 F -1 1.72 0.37 b
Mn 7 Cl -1 2.17 0.37 b
bvsparm.cif

## Slide 18
Crystal structures of some complex oxides [containing two or more cation sites]

## Slide 19
The major ternary structural families (Muller and Roy, page 3, redrawn and modified)
A3BX5
Ternary structural families
others
A2BX4
ABX4
ABX3
CaCO3
Perovskite
Hexagonal ABX3 (eg. BaNiO3 in the CsCrBr3 structure)
Pyroxenes and related structures (eg. diopside CaMgSi2O6)
Corundum and related structures (eg. ilmenite FeTiO3)
Zircon (ZrSiO4)
Scheelite (CaWO4)
Barite (BaSO4)
Ordered SiO2 derivatives
Ordered rutile derivatives
K2NiF4 (m = 1 Ruddlesden-Popper)
b–K2SO4
Olivine (Mg2SiO4 and for eg. LiFePO4)
Spinel (MgAl2O4)
CaFe2O4
Phenacite (Be2SiO4)
ABX2 (eg. LiCoO2 and CuFeO2)
A2B2X7 (eg. pyrochlore Y2Ti2O7)
A2BX5
A2BX6
not listed by Muller and Roy
Will discuss compounds in highlighted boxes: Characterized by dense connectivity.

## Slide 20
The ABO3 structure-sorting field (from Muller and Roy)
The superscripted roman numerals indicate coordination number.

## Slide 21
Perovskite
BaZrO3
LaMnO3 Pnma
(Jahn-Teller distorted)
+4/6
+2/12
Note that the space group Pnma (#62) can be written in a variety of ways.
This is the most common perovskite space group.
In the next so many structures, BO6-polyhedra are depicted.

## Slide 22
Ordered double perovskites (elpasolites), obtained through charge forking
Ba2MgWO6
Ca2MgWO6
Rock-salt like ordering of dissimilar octahedra. Space group same as rock-salt: Fm–3m
Smaller A-ions associated with tilting as in simple perovskites.
2BaZr4+O3 = Ba2(Mg2+ + W6+)O6

## Slide 23
The double perovskite field: Charge and radius
Anderson, Greenwood, Poeppelmeier, Prog. Solid State Chem. 22 (1993) 197–233.

## Slide 24
Hexagonal ABO3 structures
BaNiO3
LiNbO3 (ferroelectric R3c)
Ferroelectric YMnO3 (“YAlO3”)
Unusual 5-fold coordination (trigonal bibyramid) of MnO5

## Slide 25
Ordered rutiles (the trirutile), obtained through charge forking
CoTa2O6: 3×TiO2 = Ti3O6; 3×Ti4+ = Co2+ + 2×Ta5+

## Slide 26
The A2BO4 structure-sorting field (from Muller and Roy)
The superscripted roman numerals indicate coordination number.

## Slide 27
K2NiF4 and Ruddlesden-Popper (m = 1, 2, 3)
General formula [SrO][SrTiO3]m
Sr2TiO4
Sr3Ti2O7
Sr4Ti3O10
m = 3

## Slide 28
Spinel AB2O4
MgAl2O4
Ubiquitous structure when ions have similar sizes, around 0.6 Å.
A is tetrahedrally coordinated, and B octahedral (actually with a slight trigonal distortion).
In general, lower oxidation states and smaller bandwidths than in perovskites.

## Slide 29
Sc
Ti
V
Cr
Mn II
Fe III
Co
II
Ni
Cu
Zn
Ga
Ge
Rh
Ag
Cd
Sn
Mg
Li
Al
In
Sc
Ti III
V
III
Cr III
Mn III
Fe II,III
Co II
Ni II
Cu
Zn
Ga
Ge
Co, Rh
III
Ag
Cd
Sn
Mg
Li
Al
In
ions on the A site
ions on the B site
A,B
Jahn-Teller active
A,B
Diamagnetic
Co II
High single-ion anisotropy
Spinel AB2O4

## Slide 30
Some ABO2 structures: Highly dense in-plane, and frequently metallic
LiCoO2 (ordered rock-salt)
3R–CuFeO2 (delafossite)
111-ordered with alternating octahedral LiO6 and CoO6 stacking
BO2 (CdI2) slabs separated by two-coordinate atoms, usually Cu+ and Ag+. Also unusually, Pd1+ and Pt1+.

## Slide 31
A2B2O7 pyrochlore
6+2-coordinate A atoms and 6-coordinate B atoms.
Separately, just connecting A or just connecting B yields two interpenetrating pyrochlore lattices of corner-connected tetrahedra.
Y2Ti2O7 = Y2Ti2O6O′

## Slide 32
Some examples of the structural principles covered
https://doi.org/10.1002/anie.202000829
“Here, we test rigorously and automatically all five Pauling rules for a large data set of around 5000 known oxides… We conclude that only 13% of the oxides simultaneously satisfy the last four rules, indicating their much lower predictive power than expected.”

## Slide 33
Not the first, and not the first …
https://doi.org/110.1021/ed100258f
https://doi.org/10.1021/ed062p215

## Slide 34
Not the first, and not the first …
Letter from Pauling to W.L. Bragg. October 22, 1928:
“The last of August I sent two papers to the Editor of the Journal of the American Chemical Society. In one of them are rules governing the structures of complex crystals. I realize that nothing I have done is highly original - in particular was I gratified to read in your letter a statement of the rule governing the sharing of polyhedron elements.”

## Slide 35
O2–
O2–
Si4+
SiO2 (low quartz, P3221)

## Slide 36
O2–
O2–
O2–
O2–
P5+
Al3+
Berlinite, AlPO4, obtained structurally by forking cation charges in SiO2

## Slide 37
O22–
O12–
O12–
O22–
P5+
In3+
IPO4: In3+ is too large for 4-coordination

## Slide 38
O′2–
O2–
O2–
Cd2+
Ta5+
O2–
O2–
O2–
O2–
Ta5+
Cd2+
Pyrochlore Cd2Ta2O7: The Bond Valence Map