## Slide 1
Polar Materials and Ferroelectrics
Principles and Applications of Ferroelectrics and Related M. E. Lines, A. M. Glass. OUP Oxford, 2001
All of these materials display thermal phase transitions to a compound with a polar point group

## Slide 2
Polar Materials and Ferroelectrics
Thermal evolution of a ferroelectric
Ferroelectric soft mode: A vibration that goes to 0 frequency at the transition (upon cooling to the polar phase)

## Slide 3
Polar Materials and Ferroelectrics
From H. W. Megaw, Ferroelectricity in Crystals, Methuen, London, 1957
The original discovery by Valacek in Rochelle salt, in 1921. The Sawyer-Tower circuit for measurements is shown below.
Rochelle salt: Potassium sodium tartrate tetrahydrate, (KNaC4H4O6·4H2O)
David Brewster in 1824 demonstrated piezoelectric effects thereon, which led to him naming the effect pyroelectricity.

## Slide 4
Hydrogen-bonded ferroelectricity in Rochelle’s salt.
Polar Materials and Ferroelectrics
From H. W. Megaw, Ferroelectricity in Crystals, Methuen, London, 1957

## Slide 5
Polar Materials and Ferroelectrics
From H. W. Megaw, Ferroelectricity in Crystals, Methuen, London, 1957

## Slide 6
Hydrogen-bonded ferroelectricity in potassium dihydrogen phosphate (KDP); early neutron diffraction work.
Polar Materials and Ferroelectrics
From H. W. Megaw, Ferroelectricity in Crystals, Methuen, London, 1957

## Slide 7
Polar Materials and Ferroelectrics
From H. W. Megaw, Ferroelectricity in Crystals, Methuen, London, 1957

## Slide 8
Polar Materials and Ferroelectrics
From H. W. Megaw, Ferroelectricity in Crystals, Methuen, London, 1957

## Slide 9
Eg
A1g
Splitting of the structural soft mode (Raman active below Ta)
Ta
Antiferrodistortive transition in SrTiO3 in R-point of the Brillouin zone
Polar Materials and Ferroelectrics: SrTiO3 (on the cusp of becoming ferroelectric)

## Slide 10
Ferroelectric SM
Structural SM (doublet)
Mode frequencies on STO ceramics
(Petzelt et al., PRB 64, 184111 (2001))
Polar Materials and Ferroelectrics: SrTiO3

## Slide 11
Polar Materials and Ferroelectrics: SrTiO3

## Slide 12
Polar Materials and Ferroelectrics: SrTiO3

## Slide 13
Polar Materials and Ferroelectrics: SrTiO3

## Slide 14
Polar Materials and Ferroelectrics: SrTiO3

## Slide 15
Order-disorder model for BaTiO3 phase transitions
Dynamically disordered Ti
Ordered Ba
Polar Materials and Ferroelectrics

## Slide 16
Polar Materials and Ferroelectrics

## Slide 17
Polar Materials and Ferroelectrics

## Slide 18
Polar Materials and Ferroelectrics: Bulk and nanoscale BaTiO3
Page, Proffen, Niederberger, Seshadri, Probing local dipoles and ligand structure in BaTiO3 nanoparticles, Chem. Mater. 22 (2010) 4386–4391.

## Slide 19
Polar Materials and Ferroelectrics
Antiferroelectrics: The example of PbZrO3