## Slide 1
Oxide crystal structures: The basics
Ram Seshadri
Materials Department and Department of Chemistry & Biochemistry
Materials Research Laboratory, University of California, Santa Barbara CA 93106 USA
seshadri@mrl.ucsb.edu
Materials 218/Chemistry 277 Spring 2021

## Slide 2
en.wikipedia.org:
“Helen Dick Megaw (1 June 1907 – 26 February 2002) was an Irish crystallographer who was a pioneer in X-ray crystallography. She made measurements of the cell dimensions of ice and established the Perovskite crystal structure.”

## Slide 3
Crystal structures of simple oxides [containing a single cation site]

## Slide 4
Crystal structures of simple oxides [containing a single cation site]
N.B.: CoO is simple, Co3O4 is not. ZnCo2O4 is certainly not !
Co3O4 and ZnCo2O4 are complex oxides.
Graphs of connectivity in crystals: Atoms are nodes and edges (the lines that connect nodes) indicate short (near-neighbor) distances.
CO2: The molecular structure is O=C=O. The graph is:
Each C connected to 2 O, each O connected to a 1 C
OsO4: The structure comprises isolated tetrahedra (molecular). The graph is below:
Each Os connected to 4 O and each O to 1 Os

## Slide 5
Crystal structures of simple oxides of monovalent ions: A2O
Cu2O
Na2O (anti-fluorite)
Linear coordination is unusual. Found usually in Cu+ and Ag+.
4-coordination for Na+ and 8-coordination for O2– are unusual.

## Slide 6
Crystal structures of simple oxides of divalent ions: AO
ZnO (wurtzite), sp3
PbO (litharge), lone pairs
Pb2+ is [Xe]4f145d106s26p0
MgO (rock-salt)
Ubiquitous for AO oxides including transition metals (distorted for CuO and NbO).
Insulators, metals (TiO), magnetic, …

## Slide 7
Crystal structures of simple oxides. Al2O3 as an example of a sesquioxide
a-Al2O3 (corundum)
Also the structure of Cr2O3 and Fe2O3.
Ga2O3 does funny things.
In2O3 is different (bixbyite).

## Slide 8
B2O3 (chiral, P3121)
B2O3 (hugely important for glass industry).
NB: This structure is not in scale with the others.

## Slide 9
Crystal structures of simple oxides of tetravalent ions: AO2
TiO2 (rutile)
CeO2 (fluorite)
TiO2 also crystallizes as anatase and brookite.
SiO2 takes on this structure, and can be quenched to it, (stishovite) under pressure.
Also the structure of ThO2, and of ZrO2 and HfO2 at elevated temperatures.
Ordered variants abound.
The radius ratio rule at play:
CO2 Linear
SiO2 Tetrahedral
TiO2 Octahedral
HfO2 7-coordinate
CeO2 Cubic

## Slide 10
Oxides versus sulfides: TiS2
1T–TiS2
van der Waals gap (unlikely in oxides or fluorides, but occurs frequently in hydroxides)
This is the CdI2 structure.

## Slide 11
Crystal structures of an oxide with an octavalent ion: OsO4
OsO4

## Slide 12
Pauling’s second rule: The electrostatic valence rule
In brief: Charges going out from cations should balance anions and vice-versa
Pauling, The Nature of the Chemical Bond, 3rd Edn., Cornell University Press, Ithaca 1960
+1/2
+8/4
+3/6
electrostatic bond strength or valence
s = charge on cation/coordination number
Why is OsO4 a molecule? Radius ratio + electrostatic valence

## Slide 13
Electrostatic valence and bond valence
Pauling, and later Brown and Shannon, noted that the Pauling bond strength (the electrostatic valence) correlates very well with distance for many oxides: Short bonds (distances) correspond to strong bonds and vice-versa
Brown, Shannon, Empirical bond-strength-bond-length curves for oxides, Acta Cryst. A 29 (1973) 266–281

## Slide 14
Electrostatic valence and bond valence
The modern bond valence relationship:
Where s is the strength of the bond, R is the cation to anion distance, and R0 and B (≈ 0.37 Å) are parametrized for the specific ion pair.
When all s are calculated: valence of the ion
Brown, Shannon, Empirical bond-strength-bond-length curves for oxides, Acta Cryst. A 29 (1973) 266–281.
For Mn2+–O2–, R0 = 1.790 Å, B = 0.37 Å.
This means R = 2.20 Å.
experiment: 2.22 Å
s = +2/6

## Slide 15
Electrostatic valence and bond valence: Parameters for Mn
Mn 2 O -2 1.790 0.37 a
Mn 2 O -2 1.765 0.37 j
Mn 2 S -2 2.22 0.37 e
Mn 2 F -1 1.698 0.37 a
Mn 2 Cl -1 2.133 0.37 a
Mn 2 Br -1 2.34 0.37 e
Mn 2 I -2 2.52 0.37 e
Mn 2 N -3 1.849 0.37 j
Mn 2 N -3 1.65 0.35 e
Mn 3 O -2 1.760 0.37 a
Mn 3 O -2 1.732 0.37 j
Mn 3 F -1 1.66 0.37 b
Mn 3 Cl -1 2.14 0.37 b
Mn 3 N -3 1.837 0.37 j
Mn 4 O -2 1.753 0.37 a
Mn 4 O -2 1.750 0.37 j
Mn 4 F -1 1.71 0.37 b
Mn 4 F -1 1.63 0.37 e
Mn 4 Cl -1 2.13 0.37 b
Mn 4 N -3 1.822 0.37 j
Mn 6 O -2 1.79 0.37 e
Mn 7 O -2 1.827 0.37 e
Mn 7 O -2 1.79 0.37 b
Mn 7 F -1 1.72 0.37 b
Mn 7 Cl -1 2.17 0.37 b
bvsparm.cif

## Slide 16
Crystal structures of some complex oxides [containing two or more cation sites]

## Slide 17
The major ternary structural families (Muller and Roy, page 3, redrawn and modified)
A3BX5
Ternary structural families
others
A2BX4
ABX4
ABX3
CaCO3
Perovskite
Hexagonal ABX3 (eg. BaNiO3 in the CsCrBr3 structure)
Pyroxenes and related structures (eg. diopside CaMgSi2O6)
Corundum and related structures (eg. ilmenite FeTiO3)
Zircon (ZrSiO4)
Scheelite (CaWO4)
Barite (BaSO4)
Ordered SiO2 derivatives
Ordered rutile derivatives
K2NiF4 (m = 1 Ruddlesden-Popper)
b–K2SO4
Olivine (Mg2SiO4 and for eg. LiFePO4)
Spinel (MgAl2O4)
CaFe2O4
Phenacite (Be2SiO4)
ABX2 (eg. LiCoO2 and CuFeO2)
A2B2X7 (eg. pyrochlore Y2Ti2O7)
A2BX5
A2BX6
not listed by Muller and Roy
Will discuss compounds in highlighted boxes: Characterized by dense connectivity.

## Slide 18
The ABO3 structure-sorting field (from Muller and Roy)
The superscripted roman numerals indicate coordination number.

## Slide 19
Perovskite
BaZrO3
LaMnO3 Pnma
(Jahn-Teller distorted)
+4/6
+2/12
Note that the space group Pnma (#62) can be written in a variety of ways.
This is the most common perovskite space group.
In the next so many structures, BO6-polyhedra are depicted.

## Slide 20
Ordered double perovskites (elpasolites), obtained through charge forking
Ba2MgWO6
Ca2MgWO6
Rock-salt like ordering of dissimilar octahedra. Space group same as rock-salt: Fm–3m
Smaller A-ions associated with tilting as in simple perovskites.
2BaZr4+O3 = Ba2(Mg2+ + W6+)O6

## Slide 21
The double perovskite field: Charge and radius
Anderson, Greenwood, Poeppelmeier, Prog. Solid State Chem. 22 (1993) 197–233.

## Slide 22
Hexagonal ABO3 structures
BaNiO3
LiNbO3 (ferroelectric R3c)
Ferroelectric YMnO3 (“YAlO3”)
Unusual 5-fold coordination (trigonal bibyramid) of MnO5

## Slide 23
Ordered rutiles (the trirutile), obtained through charge forking
CoTa2O6: 3×TiO2 = Ti3O6; 3×Ti4+ = Co2+ + 2×Ta5+

## Slide 24
The A2BO4 structure-sorting field (from Muller and Roy)
The superscripted roman numerals indicate coordination number.

## Slide 25
K2NiF4 and Ruddlesden-Popper (m = 1, 2, 3)
General formula [SrO][SrTiO3]m
Sr2TiO4
Sr3Ti2O7
Sr4Ti3O10
m = 3

## Slide 26
Spinel AB2O4
MgAl2O4
Ubiquitous structure when ions have similar sizes, around 0.6 Å.
A is tetrahedrally coordinated, and B octahedral (actually with a slight trigonal distortion).
In general, lower oxidation states and smaller bandwidths than in perovskites.

## Slide 27
Sc
Ti
V
Cr
Mn II
Fe III
Co
II
Ni
Cu
Zn
Ga
Ge
Rh
Ag
Cd
Sn
Mg
Li
Al
In
Sc
Ti III
V
III
Cr III
Mn III
Fe II,III
Co II
Ni II
Cu
Zn
Ga
Ge
Co, Rh
III
Ag
Cd
Sn
Mg
Li
Al
In
ions on the A site
ions on the B site
A,B
Jahn-Teller active
A,B
Diamagnetic
Co II
High single-ion anisotropy
Spinel AB2O4

## Slide 28
Some ABO2 structures: Highly dense in-plane, and frequently metallic
LiCoO2 (ordered rock-salt)
3R–CuFeO2 (delafossite)
111-ordered with alternating octahedral LiO6 and CoO6 stacking
BO2 (CdI2) slabs separated by two-coordinate atoms, usually Cu+ and Ag+. Also unusually, Pd1+ and Pt1+.

## Slide 29
A2B2O7 pyrochlore
6+2-coordinate A atoms and 6-coordinate B atoms.
Separately, just connecting A or just connecting B yields two interpenetrating pyrochlore lattices of corner-connected tetrahedra.
Y2Ti2O7 = Y2Ti2O6O′